## Slide 1
Cleanstone Project
Carinthia University of Applied Sciences
Online Meeting, 20.05.2021
Author: FH Kärnten Team
Notes: \\

## Slide 2
Milestone 3.2 Analysis of local legislation on the disposal of stone production waste in Austria and Italy
Notes: \\

## Slide 3: White Book
WP3 MS 3.2 Austria
Legal analysis related to the disposal of stone production waste in Austria (E.C.O.)
Comparison of legal analysis in connection with the disposal of waste from stone production in Austria and Italy (Carinthian university of applied sciences)
WP3 MS 3.2 Italy
Legal analysis in relation to disposal of stone production waste in Italy (Confartigianato Vicenza)
Italy: Results Questionnaire(Confartigianato Vicenza)
Austria: Results Questionnaire (Carinthian university of applied sciences)
Comparison of the Results from the Questionnaires (Carinthian university of applied sciences)
Modification of the applicable legislation in Austria (Carinthian university of applied sciences)
Modification of the applicable legislation in Italy (Confartigianato Vicenza)
Comparison of legal modification in Austria and Italy (Carinthian university of applied sciences)
1
2
3

## Slide 4
WP4 Reuse of secondary materials as aggregates in UHPC and Normal Concrete
Notes: \\

## Slide 5: WP4 Reuse of secondary materials as aggregates in UHPC and Normal Concrete
Goal: evaluate the reusing secondary waste materials produced by the quarry sector as aggregates in:
Normal Concrete (NC) class C50/60
Ultra High-Performance Concrete (UHPC: compressive strength concrete >150MPa)
Secondary materials involved in this research:
From Crushed stone quarries: Diabas sand, Diabas powder, Dolomite sand and Dolomite gravel (AT)
From Decorative stone quarry: Marble powder (IT)

## Slide 6: NC C50/60: Secondary materials used as aggregates in Normal concrete
The amount of aggregates and parameters to calculate the concrete mixture were obtained following the recommendations of the ÖNORM B 4710-1 only as a reference since this norm does not contemplate the usage of secondary materials from quarries as aggregates for normal concrete. It was only used as a guide to calculate the amount of materials to be mixed
The ÖNORM B 4710-1 gives information of which are the best particle sizes curves for aggregates for concrete, this curves were taken as a guide to design the mixture
Secondary materials involved: Diabas Sand 0/4mm, Dolomite sand 0/4mm, Dolomite Gravel 2/4mm
As the biggest grain of the secondary materials available was Dolomite gravel 4mm, the GK4 curves were used.
The particle size curve of the mixture of the secondary materials mentioned was modified in order to fit inside the limits of the GK4 recommended curves of the ÖNORM B 4710-1 (GK4: meaning the particle size curve for concrete with a maximum grain size of 4mm)

## Slide 7: NC C50/60: Part. size curves
The red curves in the graph show the recommended limits for part. Size for concrete
By iteration of the amount of aggregates and observing how the curve was modified in comparison with the GK4 curves, the mixture of 60% of unwashed Diabas sand, 10% of Dolomite sand and 30% Dolomite gravel seemed to fit into the limit curves
The adjustment wasn’t perfect since secondary materials have a higher amount of particles passing 0,063mm sieve than recommended by the norm mentioned as it can be seen in the first part of the graph
However, the mixture was tried anyway to check if the compressive strength values were acceptable

## Slide 8: Normal Concrete Results
The final mixture was designed for a C50/60 concrete and it contained the following material amounts:
Materials | Mass (kg/m3)
CEM I 42,5 N | 550.59
Dolomite san 0/4mm | 157.16
Diabas sand 0/4mm | 942.96
Dolomite gravel 2/4mm | 471.48
H2O | 234.00
Superplasticizer | 4.40
The Compression strength show proper values for concrete C50/60. It is possible to produce Normal concrete C50/60:
Compressive strength (MPa)

## Slide 9: UHPC part. size theorical basis: Andreasen and Andersen optimal particle packing density curves
In this study, a reference mixture with commercial aggregates used in Ultra High-Performance Concrete is compared with mixtures made with secondary materials from quarries, in terms of compressive strength and workability of fresh concrete
The replacement of commercial materials by secondary ones was made following the principle of grading curves.
Therefore, the particle size distribution curves of the mixes aggregates involved were designed in order to follow the optimal particle packing density curves according to Andreasen and Andersen (A&A)

## Slide 10: UHPC: Part. Size Mixes
As the A&A curves are ideal optimal models that are difficult to reach also with commercial materials, the curves of the mixtures were intend to make as more uniform as possible, following as an example a uniform part. Size curve shape like the yellow.
The yellow curve is the UHPC part. Size curve of the company BASF in the Netherlands

## Slide 11: UHPC: reference samples. Different curing methods
Mixing optimization: the usage of an intesive mixer with higher mixing velocity instead of a mortar mixer meant higher values of compressive strength
Curing methods: Samples left in air showed less compressive streght than the ones left in water for 28 days. Samples left in hot water the first 7 days showed even better values than the others since the puzzolanic reaction is accelerated when exposed to higher temperatures (90°C). All the rest of the samples of this investigation were left in air since this reflects the real exposure of a structure and also because of energy consuming sustainable reasons

## Slide 12: UHPC: New mixes developed
Observing the results of the first batch the mixtures were modified. New ones were made:
Reference mixtures: were repeated and w/c ratio adjusted. Alternative curing methods were performed to observe the different values of compressive stregth: compressive stregth was higher by adjusting the w/c ratio and with alternative curing methods.
Designed mixes with secondary materials: w/c ratio was adjusted to get better compression strength. The amount of materials were modified in some mixtures to fit to a more uniform curve
Mixing optimization: intensive mixer was used instead of a mortar mixer since a higher velocity is required for hydration of UHPC
Coarse aggregate was tried in UHPC: Dolomite 2/4mm was added showing good results of compressive strength
The new mixtures in the graphs are the ones corresponding to the March, April and May dates

## Slide 13: UHPC: New mixes
Conclusions:
The new ref samples made in March were better than made in January and February after adjustment of w/c and mixing
The better secondary materials mixes were: JM+DS, ALL, ALL 2,5%FI, JM+DIS+DOG
The admixture of fibers didn’t change the results of compressive strength at 7 days

## Slide 14: Old mixes vs. New mixes
New mixes

## Slide 15: UHPC: Sampling and testing
Conclusions:
Mixes containing replacements of Diabas Sand and Limestone powder (Julia Marmi’s powder) show values of compressive strength that makes them suitable for producing UHPC
Admixture of coarse aggregate (Dolomite 2/4mm) showed good results of compressive strength
This offers the possibility of producing ecological friendly High-Performance concretes with the respect to a low CO2 impact of the utilized waste materials.
The usage of secondary materials avoids the dispose of them in landfills.
Stone quarry waste should be considered as secondary raw material in the concrete industry
It was possible to make Ultra High Performance Concrete only out of Secondary materials and Cement and Normal concrete C50/60
Publication: A paper about the results was already submitted to the International Multidisciplinary Scientific GeoConferences SGEM

## Slide 16: Thanks for your attention!