## Slide 1: Cleanstone Project
UNIUD- Ceramics and construction materials’ group
Maschio Stefano and Furlani Erika

## Slide 2: Materials received from “Pietra Piasentina” Consortium:
Carbonaria: cubic (100x100x100) and parallelepipedal (40x40x100) samples; slurry of waste wet powders
Julia Marmi: cubic (100x100x100) and parallelepipedal (40x40x100) samples; slurry of waste wet powders
Cudicio: cubic (100x100x100) and parallelepipedal (40x40x100) samples

## Slide 3: Investigation performed
Compressive and flexural strength tests;
Water absorption measurements;
X-Ray diffraction;
Particles size distribution of the powders derived from the slurries;
Water content of the slurries;
Optical Microscope investigation;
SEM investigation

## Slide 4: Shape of the slurries received
Water content (%): Carbonaria 41; Julia Marmi 26

## Slide 5: Results obtained
Compressive strength tests
Carbonaria: average value 147 MPa
Cudicio: average value 160 MPa
Julia Marmi: average value 170 MPa

## Slide 6: Results obtained
Flexural strength tests:
(Equation used: s f=3/2 PL/bd2)
Carbonaria: average value 26.3 MPa
Cudicio: average value 25.1 MPa
Julia Marmi: average value 33.4 MPa

## Slide 7: Results obtained
Water absorption measurements on the monoliths (% H2O)
Carbonaria: 0.030
Cudicio: 0.055
Julia marmi: 0.029

## Slide 8: X-Ray diffraction analysis
Phases identified:
Calcite 97.0 %
Quartz 1.2 %
Siderite 1.1 %

## Slide 9: Particles size distribution of the powders obtained from the slurries
Carbonaria= green
Julia marmi= red

## Slide 10: Stereoscopic optical microscope images
Carbonaria

## Slide 11: Stereoscopic optical microscope images
Carbonaria
Cudicio

## Slide 12: Stereoscopic optical microscope images
Carbonaria
Julia marmi

## Slide 13
Carbonaria
Cudicio
Julia marmi